## Slide 1: Electrochemical behavior of zirconium in molten fluoride
Tokai-mura, Ibaraki, Japan, October 24 - 26, 2018
Delphine QUARANTA1, Eric MENDES1, Laurent MASSOT2, Mathieu GIBILARO2, Jérôme SERP1
2018 International Pyroprocessing Research Conference
1 CEA Marcoule, Nuclear Energy Division, Research Department on Mining and Fuel Recycling Processes, 30207 Bagnols-sur-Cèze, France
2 Laboratoire de Genie Chimique, Université de Toulouse, UPS, CNRS, INPT, 118 Route de Narbonne, 31062, Toulouse Cedex 9, France

## Slide 2: Context Definition of Zircaloy and composition of irradiated Zircaloy cladding
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
Zircaloy
  Material constituting nuclear fuel claddings
  Main composition of Zircaloy-4
      Non-irradiated
      Irradiated claddings
Activity coming from:
      βγ elements:
        Fission products (FPs): 3H, 90Sr, 106Ru, 137Cs, 154Eu…
      Activation products (APs): 55Fe, 60Co, 59Ni, 93Zr, 94Nb, 121Sn, 125Sb
      α elements: Actinides Am, Pu, Cm, U
  Heterogeneity : distribution of radioelements, nature of elements (metal, oxide, hydrides)
Elements | Content (wt%)
Sn | 1.20 – 1.70
Fe | 0.18 – 0.24
Cr | 0.07 – 0.13
O | 0.09 – 0.16
Zr | ~ 98
Schematic of an assembly of a French nuclear fuel

## Slide 3: Context Recycling Zr contained in Zircaloy cladding
First step: fundamental comprehension of electrochemical behavior of Zr in salt
  Spent fuel management in France (La Hague reprocessing plant)
      pool storage
      shearing in 3-5 cm section
      dissolution of UO2 pellet
  Treatment of remaining Zircaloy
Aim of the study: investigation on potential recycling of Zr from irradiated Zircaloy
  → Re-use of Zr for zircaloy refabrication and/or easier storage
Identification of two promising routes
  Chemical attack at high temperature : chlorination (Collins et al. DOE, USA)
  Electrochemical processes in molten salts : electrorefining
  25 wt.% of spent nuclear fuel
Mass compositions of the constituent elements of spent nuclear fuel Collins et al. 2012
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
Geological long term Repository

## Slide 4: Experimental Setup
Cell description
Equipment
  Inactive pyrochemistry lab in gloveboxes under Ar atmosphere (< 10 ppm H2O and < 5 ppm O2)
Experimental conditions
  Temperature range 750 – 900°C
  ZrF4 concentration: 0.2 – 1.5wt%
  Electrochemical behavior and electrocrystallisation process
      Working electrode : Ag wire (1mm Ø)
      Counter electrode : glassy carbon rod (3mm Ø)
      Quasi reference electrode : Pt wire (1mm Ø)
  Electrodeposition
      Cathode : 3 different materials studied (Zr, Graphite, SS)
      Anode : Zr plates
      Quasi reference electrode : Pt wire
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
Inactive Glovebox
Salt media
  Chlorides: several stable oxidation states (0, I, II, IV) of Zr reported in the literature → Not adapted
  Fluorides: should stabilise oxidation state → Eutectic LiF-NaF

## Slide 5: Thermodynamic approach
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
pO2-
  Determination of Pourbaix diagram
      Using HSC® Chemistry database
      Considered species : Zr, ZrF4 and ZrO2
      ZrF4 activity considered: 0.1
      Limits of the diagram : reduction of Na+ and oxidation of Ag working electrode
  Influence of pO2- on stability of Zr
    Solubility limit : pKs = 24.5
    → pO2- = 11.7
    Zr very sensitive to presence of O2- in the salt
    Importance of preparation of the salt: avoiding maximum presence of oxide

## Slide 6: Electrochemical behavior: cyclic voltammetry
Cyclic voltammograms of the LiF–NaF system at 100 mV.s−1 and 750 °C: without ZrF4 (grey) and with ZrF4 addition of 0.06 mol.kg−1 (black). Inset. Variation of the peak current density (◊) and the peak potential (□) versus the square root of the potential scan rate. Working electrode: Ag (S = 0.36 cm2); auxiliary electrode: glassy carbon; comparison electrode: Pt
Reduction of Zr(IV) occurs in one step
Quasi-reversible system
Reduction is controlled by diffusion of Zr(IV)
Diffusion coefficient
Arrhenius type law →
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
      →
      →
Variation of current density of the reduction peak as a function ZrF4 molality , at 750°C and scan rate 100mV.s-1.

## Slide 7: Electrochemical behavior: square wave voltammetry
Square wave voltammogram of the LiF–NaF–ZrF4 (m0 = 0.06 mol.kg-1) at 16 Hz, pulse height: 20 mV, step potential: 2 mV and 750 °C. Inset. Variation of the differential of the peak current density (◊) and the peak potential (□) versus the square root of the frequency. Working electrode: Ag (S = 0.35 cm2); auxiliary electrode: glassy carbon; comparison electrode: Pt
Soluble/insoluble system
Reduction of Zr(IV) in one step
Number of exchanged electrons
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
4 electrons exchange

## Slide 8: Electrocrystallisation process 1/2
Chronoamperogram on silver electrode at η = −0.969V vs Pt in LiF–NaF–ZrF4 (m0 = 0.17 mol.kg−1) at 690 °C.
Working electrode: Ag (S = 0.35 cm2); auxiliary electrode: glassy carbon; comparison electrode: Pt
Chronoamperometry → 3 areas:
  Part 1: charging of the double layer and the formation of the first germs
  Part 2: growth of the crystals
  (tm ; jm) → vdiffusion = vgrowth crystals
  Part 3: limitation of the reaction by the diffusion of Zr(IV) ions
Non-dimensional models :
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
  Crossover on cyclic voltammograms observed: Nucleation process evidenced

## Slide 9: Electrocrystallisation process 2/2
Comparison of the dimensionless experimental data obtained from the current-time transients at various overvoltages and temperature with the theoretical models for instantaneous and progressive nucleation in LiF–NaF–ZrF4 (m0 = 0.17 mol.kg−1).
Working electrode: Ag; auxiliary electrode: glassy carbon; comparison electrode: Pt
Non-dimensional theoretical models → 2 nucleation modes (Scharifker et al. 1983)
  Progressive nucleation →
  Instantaneous nucleation →
Progressive nucleation mode whatever the overvoltage imposed and the working temperature
Cristal growth in the three dimensions and limited by the diffusion of Zr(IV) ions
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
Progressive nucleation: high temperature, high concentration and high overvoltage → best deposit conditions
Instantaneous Progressive
Growing speed
Growing speed
Nucleation speed
Time
Time

## Slide 10: Electrodeposition of ZR 1/4
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
ilim = -0,097A.cm-2
ilim = -0,14A.cm-2.wt%-1
Linear Voltamperogram on LiF-NaF-ZrF4 (C = 7.46.10-2mol/kg), scan range: 1mV/s at 750°C and polarisation plots.
Chronoamperograms on LiF-NaF-ZrF4 (C = 7.46.10-2mol/kg) at 750°C different applied potentials.
  Determination of the limiting current
      Fluoride media : No reference electrode
       Galvanostatic electrodeposition
      System limited by Zr diffusion
     Determination of the limiting current needed
    Tow technics: Voltammetry (low scan range) or polarisation
Higher applied current densities:
→ possible co-reduction of Na+

## Slide 11: Electrodeposition of Zr 2/4
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
SEM analysis of Zr deposited on graphite electrode in LiF-NaF-ZrF4 (C = 0.55 mol.kg-1) at 750°C, J = – 0.72 A.cm-2
Feasibility of pur Zr metal deposition demonstrated in LiF-NaF
Electrodeposition experimental results:
Anode Zr
Cathodes : Zr, C or stainless steel
Zr metal
Dendritic aspect
Consumption
Deposit loss can be observed on several experiments
Important faradic yields reached > 80%
Difficulties to estimate it (salt remaining removal)

## Slide 12: Electrodeposition of Zr 3/4
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018
XRD analysis:
  Confirmation of the SEM analysis
  Residual salt adhered onto the electrode
  Presence of oxygen: contamination of the deposit during sample preparation (under air atmosphere)

## Slide 13: Electrodeposition of Zr 4/4
Zr
C
SS
Influence of the operating parameters
Photographs of cathodes after electrolysis runs in
LiF–NaF–ZrF4 on different substrate
Photographs of cathodes after electrolysis runs in
LiF–NaF–ZrF4 at different current density
Photographs of cathodes after electrolysis runs at in LiF–NaF–ZrF4 at different molality (CA > CB)
Substrate of cathodes
Current density
ZrF4 concentration
Dense, compact and adherent deposit on Zr and C cathodes
Strong effect of current density on the regularity
Selection of the cathode material
↑ current density ↑ nuclei formed
Moderate influence of concentration on the regularity
↑ concentration ↑ nuclei formed
In good agreement with the Zr nucleation study
Deposit loss
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018

## Slide 14: Conclusions and prospects
  Electrochemical behavior in fluoride salts
      Zr(IV) reduction in one step
      Reduction is limited by diffusion of Zr(IV) ions → Arrhenius type law :
  Electrocrystallisation process
      Progressive nucleation mode
      Cristal growth
        in the three dimensions
        limited by the diffusion of Zr(IV) ions
  Electrodeposition
      Observations are in agreement with the Zr nucleation study
      → ↑current density or ↑ concentration ⇒ ↑ nuclei formed
  Next step
      Tests with non irradiated Zircaloy
2018 International Pyroprocessing Research Conference, October 24 - 26, 2018

## Slide 15: DEN DMRC SPDS LDPS
Commissariat à l’énergie atomique et aux énergies alternatives
Centre de Marcoule | 30207 Bagnols sur Cèze
T. +33 (0)4 66 79 62 51 | F. +33 (0)4 66 79 65 67
  Etablissement public à caractère industriel et commercial | RCS Paris B 775 685 019
Thank you for your attention
Acknowledgments:
Pierre CHAMELOT (LGC Toulouse)
Nicolas MASSONI (CEA Marcoule)
David RUDLOFF (CEA Marcoule)